## Slide 1: Low Rise Building No.3A UH M.Arch 18th November 2019

## Slide 2: This Presentation on GBE:
Find this file on GBE website at:
https://GreenBuildingEcyclopaedia.uk/?P=xxxxx
After the seminar/lecture I will update the page with this updated file

## Slide 3: Speaker:
Brian Murphy brianspecman@icloud.com
Technician and Architect by training, a Specification Writer by choice and an Environmentalist by action
Greening up my act since 1999
Founded National Green Specification 2001
GreenSpec.co.uk Website 2003
Started GBE online 2015 https://GreenBuildingEncyclopaedia.uk
  2050 pages created and 30,000 to go.

## Slide 4: Violet Low Rise Construction
No.3 (part) UH M.Arch 18th November 2019

## Slide 5: Conventional Low Rise 1
Masonry Cavity Wall: Brick outer block inner
  Partial or full fill cavity insulation
Ground bearing insitu concrete slab
Suspended Precast beam and Block floor
  GF sloping sites or methane/radon sites
  Upper floor Apartments (Acoustics and fire)
Suspended timber upper floors
Trussed rafter roof
Glasswool, stonewool or EPS insulated
  Will overheat
Softwood framed plasterboard partitions

## Slide 6: Conventional Low Rise 2
Masonry outer and timber framed inner Cavity Wall
  Partial or full fill cavity insulation
  stonewool or EPS insulated
Ground bearing insitu concrete slab
Suspended timber ground floor
  GF sloping or methane/radon sites
Suspended timber upper floors
Trussed rafter roof
Glasswool, stonewool or EPS insulated
  Will overheat
Softwood framed plasterboard partitions

## Slide 7: Conventional Low Rise 3
Masonry outer, light metal framed inner Cavity Wall
  Partial or full fill cavity insulation
  stonewool or EPS insulated
Ground bearing insitu concrete slab
Suspended light metal frame ground floor
  GF sloping or methane/radon sites
Suspended light metal frame upper floors
Light metal frame trussed rafter roof
Glasswool, stonewool or EPS insulated
  Will overheat
Light metal framed plasterboard partitions

## Slide 8: Conventional Low Rise 4
Masonry Solid Wall:
  Blockwork External Insulated render
Ground bearing insitu concrete slab
Suspended Precast beam and Block floor
  GF sloping sites or methane/radon sites
  Upper floor Apartments (Acoustics and fire)
Suspended timber upper floors
Trussed rafter roof
Glasswool, stonewool or EPS insulated
  Will overheat
Softwood framed plasterboard partitions

## Slide 9: Conventional Low Rise 5
SIPS Structural Insulated Panels System in place of Light timber frame
  Plastic insulation sandwich
  Roof will, walls may, overheat

## Slide 10: Conventional Low Rise 6
ICF Insulating Concrete Formwork
  Interlocking Plastic insulated formwork
  Concrete infill
  Render externally, plaster internally
  Remains vulnerable to fire
  Roof may still overheat

## Slide 11: Green Low Rise Construction
No.3 (part) UH M.Arch 18th November 2019

## Slide 12
New Build Green Materials & Construction

## Slide 13
Green Walls:
Masonry

## Slide 14
Unfired clay and straw

## Slide 15
Unfired clay
Hollow extruded clay
  Lighter weight
Interlocking profile
  Acoustic and airtight
Dry or slip clay joint
Hygroscopic
  Moisture mass
Thermal mass and lag

## Slide 16
Unfired clay and straw
Simple solid block
Straw for reinforcement and hygroscopicity
Clay mortar purpend and bed joints

## Slide 17: Cellular fired clay blocks

## Slide 18: Cellular fired clay blocks
Abundant Mineral: clay
Fired clay
Cellular insulation
Long conduction path
Interlocking dry perpend
Mortared bed joint
Thermal mass
Acoustic mass
Decrement delay
Moisture Permeable

## Slide 19: Cellular fired clay blocks
Knock out pieces
Allow conduit runs
Form corners and interlocking

## Slide 20
Thermal mass:
Fired honeycomb
blocks in walls and floors adds long term thermal and acoustic mass
Clay board adds short term thermal mass
Not high load capacity
Construction Resources Showrooms Southwark London
Thermal Mass

## Slide 21: 21st Century Cob Walls
CobBauge Interreg Channel Project
Phase 2 underway
Traditional will not meet BRADL
Structural Cob + Insulating Cob
600 mm U value: 0.28 W/m2.K (0.3min)
U: 0.15 achievable CobBauge Phase3

## Slide 22: CobBauge
2 halves make a whole
Structural k=0.42
Insulating k=0.11
Act as one
Difficult to get apart
400 mm wall shown

## Slide 23: Hemp-Lime
Hempcrete
Hemp shiv (part of stalk)
  is aggregate in a mix
Lime
  (lower energy and carbon than Cement)
Mixed to a concrete-like mix
  Sprayed into open cassettes or like render
  Cast into formwork and tamped down

## Slide 24: 21st Century hemp-lime
Hemcrete via Lime Technology Ltd. Tradical by Lhoist (FR)
Hemp shiv: part of stalk
  is aggregate in a mix
Lime
  Lower energy and carbon than Cement
Cement
  Higher energy and carbon than Lime
  To get an initial set sooner
  To drive the lime to hydrate faster
Aluminium Oxide
  High embodied energy and carbon
  Chemical reaction with cement: Saponificate: Bubbles entrained in cement matrix
Mixed to a aerated concrete-like mix
  Sprayed into open cassettes or like render
  Cast into formwork and tamped down
  Into robust CLT Frame
  Air pushed through to hydrate and dry mix for quick turn around
  MMC Moderns Method of Construction or IMC Innovative Method of Construction

## Slide 25
Green Walls:
Timber

## Slide 26: EVT Enhanced Vapour Transfer
Hygroscopic insulation
maintain their performance
even when moist
Vapour and water released
when conditions permit
No need for VB Vapour Barrier
Use vapour permeable
construction
5:1 ratio vr inside:outside
ATL air tightness layer
Construction Resources Showrooms Southwark London

## Slide 27
Hygroscopic insulation
maintain their performance
even when wet
Vapour and water released
when conditions permit
No need for Vapour Barrier VB
Use vapour permeable
construction
5:1 ratio vr inside:outside
Air Tightness Layer ATL
Not for High Rise/near boundary
Construction Resources Showrooms Southwark London
EVT Enhanced Vapour Transfer

## Slide 28
We have a preoccupation with
thin walls 300 mm. or less
Which drives the demand for
energy intensive man-made
petrochemical fossil derived
CFC HCFC HFC HFA foamed plastic
O3 Ozone Depletion
Greenhouse Gas Potential
300-600 mm. optimum
insulation thicknesses
Construction Resources Showrooms Southwark London
Thick walls, roofs and floors

## Slide 29
Optimum:
300-400 mm. deep compound rafters with Cellulose fibre
insulation
High density and
high thermal mass
cellulose fibre insulation
boards in walls and floors
Construction Resources Showrooms Southwark London
Cellulose Fibre

## Slide 30
Thermal mass:
High thermal mass dense wood fibre insulation boards in walls and floors
Acoustic unfired clay bricks in floor construction
adds thermal and moisture mass
Stacked dowelled wood floor
No glue: healthy
Construction Resources Showrooms Southwark London
Thermal Mass

## Slide 31
Thermal mass:
High thermal mass dense wood fibre insulation boards in walls and floors
Acoustic unfired clay bricks in floor construction or fired
honeycomb
blocks in walls
and floors adds
thermal mass
Construction Resources Showrooms Southwark London
Thermal Mass

## Slide 32
Compound rafters
Cellulose insulation
Acoustic brick floor
Timber floor planks
Wood fibre insulation
Timber frame walls
Timber batten clad
Vapour balanced construction
Construction Resources Showrooms Southwark London
Timber Structure

## Slide 36
Green Walls:
Loadbearing Timber Blocks

## Slide 37
STEKO
Load-bearing timber blockwork
Construction Resources Showrooms Southwark London

## Slide 38
STEKO
Load-bearing timber blockwork

## Slide 39: Steko “Lego for Self-builders”
Waste from plantation thinning
Carbon negative
  Carbon sequestration
Dry Construction
Self-build unskilled construction
Fast construction (3 day house)
No waste on site (designed)
Accommodates services
Accommodates thermal or acoustic insulation
Lightweight 6kg (children too)
Load-bearing (designed to 7 stories)
Internal and external walls
160 mm. modules

## Slide 42: Cross Laminated Timber Panel (CLTP) Low & High rise

## Slide 43
Cross Laminated timber shear walls floors and roofs

## Slide 44
Cross Laminated timber shear walls floors and roofs

## Slide 45: Post Grenfell fire
Government Announced combustible materials no longer permitted in High rise Housing above 18m
2 Different interpretations
  Not in the external wall
    (replaced with LSF and Stone wool)
  Not at all
    Back to concrete
Sector challenging Government because timber and CLTP has predictable behaviour in fire
  Difficult to set CLTP alight
    Small sections easy
  Known charring rate thickness/minute
  Charring protects remainder of big sections

## Slide 46
Cross Laminated timber walls

## Slide 47: Post Grenfell fire
Government Announced combustible materials no longer permitted in High rise Housing above 18m
Stone wool e.g. Rockwool could be the only insulation player in the market (no more plastics)
I have challenged the dense wood fiber (DWF) insulation sector to do the tests to prove their insulation is up to the job of high rise housing
  Difficult to set DWF alight with blowtorch
  Some charring at surface
  Charring protects remainder of insulation
Expensive tests but informally Austrian manufacturers and UK suppliers progressing

## Slide 48: Cross Laminated timber shear walls

## Slide 49
Green New Walls: Transparent

## Slide 50: Timber Curtain Walling

## Slide 51: Solar Wall

## Slide 52
Green
Wall Finishes

## Slide 53: Rammed Earth Walls
any shape
many ingredients
colours & textures
thermal mass
Load-bearing
but dynamic

## Slide 54: Rammed Earth Walls
Abundant and Natural
Recipe can be determined on site
Thermal, Acoustic & Moisture mass
Fire resistant
Load-bearing
Absorbs radiation, smells and moisture
Hygroscopic
Any shape
many ingredients, colours & textures
Sculptural & Artistic opportunities
Waste disposal back to earth
Recyclable & Reusable
Needs temporary formwork

## Slide 55: Clay boards & finishes
Clay Boards
Reed & Clay
Clay finishes
Construction Resources Showrooms Southwark London

## Slide 56: Clay Finishes
Construction Resources Showrooms Southwark London
Clay Boards: Reed & Clay,
Insitu clay on reed
Clay finish
Dry and harden but do not set
No time limits
Easy repairs
Less skill required

## Slide 57: Clay Finishes
Construction Resources Showrooms Southwark London
Can sustain high humidity where gypsum/paper will harbour mould
  Hygroscopic
  Moisture Mass
  Condensation avoidance
  Mould avoidance
Thermal mass
  High density
  Large surface area
Electromagnetic radiation absorption
Absorbs smells

## Slide 58: Clay finishes
Construction Resources Showrooms Southwark London
Mineral based dies
Non-fade
Bond to background
No flaking
Long life
Durable
Properties of clay plaster
Vapour permeable

## Slide 59: Paints & Stains
Natural
ingredient
Paints
Stains
Oils
Waxes
Polishes
Sealers
Construction Resources Showrooms Southwark London

## Slide 60: Natural Paints
No synthetics
  VOCs if any are natural
No poisons
No chemical concoctions
  No unexplored impacts or reactions
No pollutants
  Healthy career possible
No Hazardous waste
  Many compostable

## Slide 61
Green Acoustic Construction

## Slide 62: Different Acoustic solutions to walls and floors Cavity and solid walls and lightweight partitions

## Slide 63: Acoustic Separating Floor
Floor board/Sheet
Isolation felt
Acoustic massive unfired clay bricks laid loose
Perimeter coconut fibre upstand
Isolation felt
Floor deck/sheet
I-Joist stiff floor structure
Acoustic insulation in void
Acoustic insulation at floor edge
Isolation suspension fixing
Dense Cellulose fibre reinforced gypsum board ceiling

## Slide 64: Acoustic Party Wall
Blockwork cavity wall
Isolation rubber strip in place of mortar positioned mid floor depth to minimise flanking sound
Airtight plaster on both faces of room walls
Acoustic insulation in party wall cavity, extends into floor zone

## Slide 65: Acoustic Intermediate Floor
Carpet
Cork/rubber crumb or wood fibre sheet acoustic underlayment
Or Rubber sheet
Floor board/Sheet
Softwood joists
Close to party wall but spaced off with wedges
Noggins to support ceiling joints
2 layers dense cellulose fibre reinforced gypsum board ceiling

## Slide 66: Intermediate Floor
Veneered timber panel floor boarding
wood fibre sheet acoustic underlay
wood fibre board acoustic/thermal insulation
wood fibre sheet acoustic underlayment and upstand
Stacked wood floor with acoustic absorbent slotted soffit
Isolation rubber strip in place of mortar positioned below and above solid timber floor to minimise vibrations transfer from floor to wall and minimise flanking sound

## Slide 67: Intermediate Wall
Blockwork cavity wall
Isolation rubber strip in place of mortar positioned below and above solid timber and insitu concrete floors to minimise vibrations transfer from floor to wall and minimise flanking sound
Insulation in cavity to minimise flanking sound

## Slide 68: Intermediate Floor
Carpet
Screed could contain recycled aggregates and GGBS cement
Damp and vapour proof membrane
coconut fibre sheet acoustic underlayment and upstand
Insitu concrete floor with fairfaced soffit exposing thermal mass
Isolation rubber strip in place of mortar positioned below and above insitu concrete floor to minimise vibrations transfer from floor to wall and minimise flanking sound

## Slide 69: Acoustic Intermediate Floor
Ceramic floor tiles
2 layers of underlayment
Floor board/Sheet
Softwood joists
Close to party wall but spaced off with wedges
Noggins to support ceiling board joints
2 layers dense cellulose fibre reinforced gypsum board ceiling

## Slide 70: Acoustic Internal partition
Single leaf blockwork
Plastered & Skirting
Parge coated for airtightness
Dense wood fibre board drylined on dabs
Plaster skim & Skirting
Battens acoustic insulation between
Dense cellulose fibre reinforced gypsum board

## Slide 71: Acoustic Intermediate Floor
Carpet
Underlayment
Floating Floor board/Sheet
Acoustic insulation
interlocking Hollow timber beam floor
Acoustic insulation at wall abutment
Exposed soffit

## Slide 72: Acoustic Suspended Floor
Carpet
Screed could contain recycled aggregates and GGBS cement
Damp and vapour proof membrane
coconut fibre sheet acoustic underlayment and upstand
Insitu concrete floor with fairfaced soffit

## Slide 73: Acoustic Partition (below)
Multi layered timber framing acoustic isolation
dense cellulose fibre acoustic insulation between battens
dense cellulose fibre reinforced gypsum board

## Slide 74: Acoustic Suspended Floor
Carpet
2 layers of underlayment dense cellulose fibre reinforced gypsum board
Monolithic topping could contain recycled aggregates and GGBS cement
Insitu concrete floor with fairfaced soffit
Acoustic bridge through partition

## Slide 75
Victorian Building Green Energy Upgrade

## Slide 76: Solid Wall Construction
Eco Energy Refurbishment
9 in brick wall
Plastered internally
Cork insulation
In two layers
cross battens
To reduce thermal
Bridge through battens
Drylined
Skirting

## Slide 77: Pitched roof Construction
Eco Energy Refurbishment
Existing rafter zone insulated leaving 50 mm. ventilation zone
Cross battens applied below rafters, batten zone insulated
Plasterboard ceilings added

## Slide 78: Suspended Ground Floor
Eco Energy Refurbishment
Battens to sided of floor joists
Board on battens
Insulation onto boards
Existing floor joist zone insulated

## Slide 79: Suspended Upper Floor
Eco Energy Refurbishment
Ceiling joists upgraded to floor joist
Joist zone insulated
Floor boards added
Ceiling linings

## Slide 80: Aerogels
Minerals e.g. Silica in solution
Remove the water and you have microscopic air cells held together by the mineral
Higher performance than the best foamed plastics (k value)
Used attached to boards or in a board sandwich
Wall and floor linings
Used in DGSU translucent GRP glazing

## Slide 81
20th C Building Green Energy Upgrade

## Slide 82: Cavity Wall Construction
Eco Energy Refurbishment
Existing masonry cavity wall,
Brick outer leaf, block inner leaf,
Steel lintel thermal bridge plastered internally;
Insulate cavity
Internal insulation
Wrap lintel
Plasterboard dry lining

## Slide 83: Pitched Roof Attic
Eco Energy Refurbishment
Existing ceiling joists zone insulated
Insulation laid over ceiling joists at right angles

## Slide 84: Ground floor
Eco Energy Refurbishment
Take up existing floor
Lay new DPM
Loadbearing Insulation on DPM
Insulation upstand around perimeter
New eco-concrete floor,
Eco-concrete screed
High density insulation board
Floor finish

## Slide 85: 1960’s insitu concrete tower refurbishment External walls
Eco Energy Refurbishment

## Slide 86: 1960’s insitu concrete tower refurbishment Flat roof gutter
Eco Energy Refurbishment

## Slide 87: 2015
If we have not made significant changes by 2015
2050 is melt down day
The one planet will survive
Unable to support humans living a three planet lifestyle
  UK average citizen

## Slide 88
Another GBE CPD/Lecture to download
And https://greenbuildingencyclopaedia.uk

## Slide 89: Sampler
This is a cut down version of the original file to give you a sample of the whole
It’s the front end of the file with the middle and rear end deleted
Go to https://GreenBuildingEncyclopaedia.uk
to down load the whole file
You will find a large number of other files there too

## Slide 90: Feedback
These files are created by generalists with a big dollop of green flavour
These files are updated from time to time
We are not experts so from time to time these file may get out of date or may be wrong.
If you feel that we have got it wrong please let us know so we can put it right

## Slide 91: © GBE 2003 - 2019
Brian Murphy BSc Dip Arch (Hons+Dist)
  Technician and Architect by Training
  Specification Writer by Choice
  Environmentalist by Actions
Greening up my act since 1999
Founded National Green Specification 2001
Launched www.greenspec.co.uk 2003
Created: GBE at https://greenbuildingencyclopaedia.uk 2015
E BrianSpecMan@icloud.com
Twitter: http://twitter.com/brianspecman
LinkedIn: BrianSpecMan
Facebook: http://www.facebook.com/brianspecman
Slide Share:
Pinterest: Brian Murphy • GBE Green Building Encyclopaedia